## Slide 1
Nanoparticle Synthesis and Applications

## Slide 2: Outline
Nanoparticle Synthesis
  Colloidal Chemical Methods
  Attrition
  Pyrolysis
  RF Plasma
  Thermal decomposition
  Pulsed Laser Method
Some Nanoparticle Applications

## Slide 3: Colloidal Methods
Colloidal chemical methods are some of the most useful, easiest, and cheapest ways to create nanoparticles.
Colloidal methods may utilize both organic and inorganic reactants.
Typically, a metal salt is reduced leaving nanoparticles evenly dispersed in a liquid.
Aggregation is prevented by electrostatic repulsion or the introduction of a stabilizing reagent that coats the particle surfaces.
Particle sizes range from 1-200nm and are controlled by the initial concentrations of the reactants and the action of the stabilizing reagent.

## Slide 4: Colloidal Methods
Examples: Gold
  A common method for preparing colloidal gold nanoparticles involves combining hydrogen tetrachloroaurate (HAuCl4) and sodium citrate (Na3C6H5O7) in a dilute solution.
  Upon dissociation, the citrate ions (C6H5O73-) reduce Au3+ to yield 30-40 nm gold particles.
  Half reaction equations:
    Au3+(aq) + 3e-  Au(s)
    C6H5O73-(aq) +H2O(l)  C5H4O42-(aq) + CO2(g) + H3O(aq) + 2e-

## Slide 5: Example: Formation of Gold Nanoparticles
HAuCl4
Gold
NP
HAuCl4
Sodium
Citrate
Heat
http://mrsec.wisc.edu/Edetc/nanolab/gold/index.html
J. Chem. Ed. 2004, 81, 544A.
Heat a solution of chloroauric acid (HAuCl4) up to reflux (boiling). HAuCl4 is a water soluble gold salt.
Add trisodium citrate, which is a reducing agent.
Continue stirring and heating for about 10 minutes.
  During this time, the sodium citrate reduces the gold salt (Au3+) to metallic gold (Au0).
  The neutral gold atoms aggregate into seed crystals.
  The seed crystals continue to grow and eventually form gold nanoparticles.
Red Color = Gold NP

## Slide 6: Example: Formation of Gold Nanoparticles
Reduction of gold ions: Au(III) + 3e- → Au(0)
Nucleation of Au(0) seed crystals:
Seed Crystal
10’s to 100’s of Atoms
Nanorods
Spherical
Nanoparticles
Isotropic
Growth
Anisotropic
Growth
Surface capped
with citrate anions
Adding surfactant to growth solution
caps certain crystal faces and promotes
growth only in selected directions.
Growth of nanoparticles:
Seed

## Slide 7: Colloidial Methods
Examples: Molybdenum
  1-5 nm molybdenum nanoparticles can be created at room temperature by reducing MoCl3 in a toluene solution in the presence of sodium triethylborohydride (NaBEt3H).
  Reaction equation:
  MoCl3 + 3NaBEt3H  Mo + 3NaCl + 3BEt3 + (3/2)H2

## Slide 8: Colloidal Methods
Examples: Iron
  The TEM image to the right shows 3nm Fe nanoparticles produced by reducing FeCl2 with sodium borohydride (NaBH4) in xylene.
  Trioctylphosphine oxide (TOPO) was introduced as a capping agent to prevent oxidation and aggregation
Phys. Chem. Chem. Phys., 2001, 3, 1661È1665
TEM image of Fe nanoparticles

## Slide 9: Colloidal Methods
Examples: Silver
  The reduction of AgNO3 by NaBH4 in aqueous solution can produce small diameter (<5nm) silver nanoparticles
  In one reported method, the reduction takes place between layers of kaolinite, a layered silicate clay material that functions to limit particle growth.
  Dimethyl sulfoxide (DMSO) is used as a capping agent to prevent corrosion and aggregation of the Ag particles.
R. Patakfalvi et al. / Colloids and Surfaces A: Physicochem. Eng. Aspects 220 (2003) 45/54

## Slide 10: Attrition
Attrition is a mechanical method for creating certain types of nanoparticles.
Macro or micro scale particles are ground in a ball mill, a planetary ball mill, or other size reducing mechanism.
The resulting particles are separated by filters and recovered.
Particle sizes range from tens to hundreds of nm.
Broad size distribution and varied particle geometry.
May contain defects and impurities from the milling process.
Generally considered to be very energy intensive.
Cao, Guozhong. Nanostructures and Nanomaterials: Synthesis, Properties & Applications. Imperial College Press. 2004

## Slide 11: Attrition: Rotary Ball Mill
A hollow steel cylinder containing tungsten balls and a solid precursor rotates about its central axis.
Particle size is reduced by brittle fracturing resulting from ball-ball and ball-wall collisions.
Milling takes place in an inert gas atmosphere to reduce contamination.
http://www.ktf-split.hr/glossary/image/ball_mill.gif

## Slide 12: Attrition
Attrition Examples
Claudio L. De Castro, Brian S. Mitchell. Nanoparticles from Mechanical Attrition.
Department of Chemical Engineering, Tulane University, New Orleans, Louisiana, USA

## Slide 13: Outline
Nanoparticle Synthesis
  Colloidal Chemical Methods
  Attrition
  Pyrolysis
  RF Plasma
  Thermal Decomposition
  Pulsed Laser Method
Nanoparticle Applications

## Slide 14: Pyrolysis
History
System Overview
Aggregation and agglomeration
Impact of oxygen flow
Jet design
Flame quenching
    Nozzle quenching
    Electrostatic Charging

## Slide 15
Pyrolysis: Material Applications
Images clockwise from top left:
1. Tire <www.Safercar.gov>
2. Paint cans <http://www.ndhealth.gov/wm/PollutionPreventionAndRecyclingProgram/ MercuryContainingDevicesProducts.htm>
3. Optical Fibers <https://lasers.llnl.gov/publications/photons_fusion/2009/january
_february.php>
4. Vitamans <www.fda.gov/AboutFDA/WhatWeDo/History/ThisWeek/ucm117726.htm>
5. Makeup <https://pa-online.pa.gov.sg/NASApp/sdsol/sdsol/common
/Bring_Out_Best_In_You.htm>
6. Ink Quil < http://www.orovalleyaz.gov/Town_Government/Town_Clerk/notary_services.htm>
Carbon Black
TiO2
SiO2
Tires
Inks
Paints
Makeup
Flowing aid
Optical
fibers

## Slide 16: Annual Production of Flame made materials
Carbon black – 8 million tons $8 billion
TiO2 - 2.5 million tons, $5 billion
SiO2 2.0 million tons, $2 billion

## Slide 17
Pratsinis, Sotiris E., Functional Nanoparticles and Films Made in the Gas-phase. Nano Science and Technology Institute, Cambridge. 2008

## Slide 18
Pratsinis, Sotiris E., Functional Nanoparticles and Films Made in the Gas-phase. Nano Science and Technology Institute, Cambridge. 2008

## Slide 19: Pyrolysis
Pyrolysis is a popular method for creating nanoparticles, especially oxides. A precursor (liquid or gas) is forced through an orifice at high pressure and burned.
The resulting ash is collected to recover the nanoparticles.
Large volume of gas leads to high rate of material synthesis

## Slide 20
Flame Spray Pyrolysis (FSP)
Versatile
Large Variety of precursors
Controllable
Scalable
Aggregation
Condensation
Coagulation
Nucleation
Droplet evaporation

## Slide 21: Pyrolysis: System Overview
Xiao Q., Yiguang J., Stefan B. and Nan Y. Synthesis of Y2O3:Eu Phosphor Nanoparticles by Flame Spray Pyrolysis. Princeton University, Princeton, NJ

## Slide 22
Pyrolysis
Aggregates and Agglomerates:
Aggregate – An assemblage of particles rigidly joined together by chemical or sinter-forces.
Agglomerate – A loosely coherent assembly of particles and/or aggregates held together by weak interactions
Current aerosol instruments cannot distinguish between them.
  Aggregates Agglomerates

## Slide 23
Pyrolysis
Agglomerate Formation Sequence
Residence time
TiO2
Monomers
Transient Hard
Agglomerates
Spherical
Particles
Hard Agglomerates
Soft Agglomerates

## Slide 24
Pyrolysis
Degree of agglomeration matters:
Agglomerated
  Fillers
  Catalysts
  Lightguide preforms
  Particles for CMP
Non-agglomerated
  Pigments
  Composites
  Electronics
Distinction between hard and soft agglomerates is largely empirical.
Controlled agglomeration can minimize post-grinding and other costly separation techniques.
Pratsinis, Sotiris E., Functional Nanoparticles and Films Made in the Gas-phase. Nano Science and Technology Institute, Cambridge. 2008

## Slide 25
Pyrolysis
Regions of Agglomeration
Non-Agglomerates
Hard Agglomerates
Soft Agglomerates
Pratsinis, Sotiris E., Functional Nanoparticles and Films Made in the Gas-phase. Nano Science and Technology Institute, Cambridge. 2008

## Slide 26
Pyrolysis

## Slide 27
Impact of oxygen
Aids in combustion
Provides chemistry in the reaction
Acts as a dilutent, cools the flame, prevents agglomeration
All of these variables can be decoupled by burner design. Which is cheaper than increasing oxygen flow.
Pyrolysis

## Slide 28
Pyrolysis
Particle Size Controlled by O2 Flow
Excess oxygen makes the flame burn cooler resulting in smaller diameter particles

## Slide 29
Pyrolysis
Particle Formation and Growth by Gas Phase Chemical Reaction, Coagulation, Sintering and Surface Growth:
O2
TTIP
Molecules
TiO2
Molecules
TiO2
Particles
Ti
C3H7O
C3H7O
OC3H7
OC3H7
Titanium-Tetra-Iso-Propoxide
TiO2
Aggregates
Decreasing Temperature
Pratsinis, Sotiris E., Functional Nanoparticles and Films Made in the Gas-phase. Nano Science and Technology Institute, Cambridge. 2008

## Slide 30
Pyrolysis: Jet Design
CH4
CH4
CH4
Air
Air
Air
TiCl4
TiCl4
TiCl4
TiCl4
Air
Air

## Slide 31
Pyrolysis: Jet Design
Effect of Oxidant Composition on TiO2 Morphology:
CH4
CH4
Oxidant
Oxidant
TiCl4
TiCl4
Flame mixing B
Flame mixing C

## Slide 32
Pyrolysis: Nozzle Quenching
Pratsinis, Sotiris E., Functional Nanoparticles and Films Made in the Gas-phase. Nano Science and Technology Institute, Cambridge. 2008
Vapor
Flame length is controlled by rapid quenching
Prevents agglomeration by inhibiting growth processes in the early stages of growth.
Provides precise control of particle size
Desired

## Slide 33
Pyrolysis: Nozzle Quenching
Nozzle Quenching controls flame length and particle size.

## Slide 34
Pyrolysis: Nozzle Quenching
TiO2 Particle Size Control by Nozzle Quenching
Pratsinis, Sotiris E., Functional Nanoparticles and Films Made in the Gas-phase. Nano Science and Technology Institute, Cambridge. 2008

## Slide 35
Pyrolysis: Electrostatic Charging
Particle size can also be controlled by generating an electric field across the flame.
A large electric field (hundreds of kV/m) is generated between two plate electrodes situated on opposite sides of the flame.
Similar to nozzle quenching, the electric field limits particle growth by reducing the residence time in the high temperature region of the flame.
In addition, the electric field charges the particles. This results in electrostatic repulsion between newly formed particles, preventing coagulation.
S. Vemury, S.E. Pratsinis, L. Kibbey, Electrically-controlled flame synthesis of nanophase TiO2, SiO2, and SnO2 powders. JMR, Vol. 12, 1031-1042. 1997.

## Slide 36
Pyrolysis: Electrostatic Charging

## Slide 37
Pyrolysis is a high yield method that can fulfill the strong demand for nanoparticles.
Can be customized to produce unique nanoparticles.
Broad distribution of particle sizes and morphology.
Pyrolysis: Advantages & Disadvantages

## Slide 38: Outline
Nanoparticle Synthesis
  Colloidal Chemical Methods
  Attrition
  Pyrolysis
  RF Plasma
  Thermal Decomposition
  Pulsed Laser Method
Nanoparticle Applications

## Slide 39: RF Plasma Synthesis
The starting material is placed in a pestle and heated under vacuum by RF heating coils.
A high temperature plasma is created by flowing a gas, such as He, through the system in the vicinity of the coils.
When the material is heated beyond its evaporation point, the vapor nucleates on the gas atoms which diffuse up to a cooler collector rod and form nanoparticles.
The particles can be passivated by introducing another gas such as O2.
In the case of Al nanoparticles the O2 forms a thin layer of AlO3 around the outside of the particle inhibiting aggregation and agglomeration.
RF plasma synthesis is very popular method for creating ceramic nanoparticles and powders
Low mass yield.
Poole, C., Owens, F. Introduction to Nanotechnology. Wiley, New Jersey. 2003

## Slide 40: RF Plasma Apparatus
Poole, C., Owens, F. Introduction to Nanotechnology. Wiley, New Jersey. 2003

## Slide 41: Thermal Decomposition
  Thermal decomposition is the chemical decomposition of a substance into ins constituents by heating.
  A solid bulk material is heated beyond its decomposition temperature in an evacuated furnace tube.
  The precursor material may contain metal cations and molecular anions, or metal organic solids.
  Example: 2LiN3(s) 2Li(s) +3N2(g)
  Lithium particles can be synthesized by heating LiN3 in a quartz tube under vacuum.
  When heated to 375oC the nitrogen outgases from the bulk material and the Li atoms coalesce to form metal nanoparticles.
Poole, C., Owens, F. Introduction to Nanotechnology. Wiley, New Jersey. 2003

## Slide 42: Thermal Decomposition Apparatus
Sample in Ta foil
Furnace
Evacuated
Quartz Tube
Turbo Molecular
Pump
Mechanical Pump

## Slide 43: Outline
Nanoparticle Synthesis
  Colloidal Chemical Methods
  Attrition
  Pyrolysis
  RF Plasma
  Thermal Decomposition
  Pulsed Laser Methods
Nanoparticle Applications

## Slide 44: Pulsed Laser Methods
Pulsed Lasers have been employed in the synthesis silver nanoparticles from silver nitrate solutions.
A disc rotates in this solution while a laser beam is pulsed onto the disc creating hot spots.
Silver nitrate is reduced, forming silver nanoparticles.
The size of the particle is controlled by the energy in the laser and the speed of the rotating disc.
Poole, C., Owens, F. Introduction to Nanotechnology. Wiley, New Jersey. 2003

## Slide 45: Pulsed Laser Apparatus for Ag Nanoparticles
Poole, C., Owens, F. Introduction to Nanotechnology. Wiley, New Jersey. 2003

## Slide 46: Nanoparticle Applications: ZnO
Zinc Oxide has opaque and antifungal properties.
Used as UV blocking pigments in sunscreens, cosmetics, varnishes, and fabrics
Incorporated in foot powders and garden supplies as an antifungal.
ZnO nanowires can improve the elastic toughness of bulk materials

## Slide 47: Nanoparticle Applications: TiO2
Titanium Dioxide is used as an inorganic white pigment for paper, paints, plastics, and whitening agents.
TiO2 nanoparticles are used as UV blocking pigments in sunscreens, cosmetics, varnishes, and fabrics.
TiO2 has unique photocatalytic properties that make it suitable for a number of advanced applications:
  Self-cleaning glass and antifogging coatings
  Photoelectrochemical cells (PECs)
  Detoxification of waste water
  Hydrolysis

## Slide 48: Nanoparticle Applications: Fe
50-100nm Iron nanoparticles are used in magnetic recording devices for both digital and analog data.
Decreasing the diameter to 30-40nm increases the magnetic recording capacity by 5-10 times per unit.

## Slide 49: Nanoparticle Applications: Iron Oxide
Iron Oxide nanoparticles have unique magnetic and optical properties.
Iron oxide nanoparticles can be translucent to visible light while being opaque to UV light.
Applications include UV protective coatings, various electromagnetic uses, electro-optic uses, and data storage.

## Slide 50: Nanoparticle Applications: Iron Alloys
Iron-platinum nanoparticles have increased magnetism and it is predicted that 3nm particle can increase the data storage capacity by 10 times per unit area.
Iron-palladium nanoparticles 100-200nm in diameter have been shown to reduce toxic chlorinated hydrocarbons to nontoxic hydrocarbon and chloride compounds.
SCIENCE VOL 287 17 MARCH 2000

## Slide 51: Nanoparticle Applications: Alumina
Alumina (Aluminum Oxide) is used in Chemical Mechanical Polishing (CMP) slurries, as well as ceramic filters.
Nano-alumina is used in light bulb and fluorescent tube coatings because it emits light more uniformly and allows for better flow of fluorescent materials.

## Slide 52: Nanoparticle Applications: Ag
Silver has excellent conductivity and has been used as an antimicrobial material for thousands of years.
Silver’s anti-microbial potential increase with increased surface area.
Applications include biocides, transparent conductive inks, and antimicrobial plastics, and bandages.

## Slide 53: Nanoparticle Applications: Gold
Gold nanoparticles are relatively easy to produce compared to other types of nanoparticles due to its high chemical stability.
Uses for gold nanoparticles are typically catalytic and include DNA detection and the oxidation of carbon monoxide.
Gold has superior conductivity allowing gold nanoparticles to be used in various probes, sensors, and optical applications.

## Slide 54: Nanoparticle Applications: Gold
The First Response® home pregnancy test uses 1µm polystyrene sphere and 50nm gold particles coated with an antibody to human chorionic gonadotropin (hCG), a hormone produced during pregnancy.
When urine containing hCG comes in contact with the polystyrene-gold-antibody complex, the nanoparticles coagulate into red clumps. Fluids pass through a filter where the clumps are caught yielding a pink filter.
Suspended (un-coagulated) nanoparticles pass through the filter and no color change occurs.
Bangs, L. B. New Developments in Particle-based Immunoassays. Pure & Appl. Chem. Vol. 68, No 10 p 1873-1879. 1996

## Slide 55: Nanoparticle Applications: Gold
Bangs, L. B. New Developments in Particle-based Immunoassays. Pure & Appl. Chem. Vol. 68, No 10 p 1873-1879. 1996

## Slide 56: Nanoparticle Applications: ZrO
Zirconium Dioxide nanoparticles can increase the tensile strength of materials when applied as a coating.
This has many possible applications in wear coatings, ceramics, dies, cutting edges, as well as piezoelectric components, and dielectrics.