## Slide 1
Light Trapping

## Slide 2: Outline
Flat solar cells
  ARC for flat solar cells
  Manifestations of Fabry Perot Resonances
Light trapping
  Advantage of a nanodome
  Yablonovitch limit
  Bloch modes
  Diffraction aided waveguiding
  Mie resonances
  Hybridizations
  Plasmonics
Examples

## Slide 3: Flat Solar Cells Antireflection Coating
ARC (60nm)
t
ZnO
PbS
metal
light

## Slide 4: Flat Solar Cells: Manifestations of Fabry Perot Resonances
light
t1=100nm
t2=500nm
Au
PbS (absorber)
ZnO
r: radius
h: height
L: period

## Slide 5: Flat Solar Cells: Manifestations of Fabry Perot Resonances
r/h
What can be the sources of these peaks?

## Slide 6: Flat Solar Cells: Manifestations of Fabry Perot Resonances
Resemblance?

## Slide 7: Flat Solar Cells: Manifestations of Fabry Perot Resonances
200nm
500nm
800nm

## Slide 8: Flat Solar Cells: Manifestations of Fabry Perot Resonances
t1
t2

## Slide 9: Flat Solar Cells: Manifestations of Fabry Perot Resonances
Shift Rpeak
Flat cells: Increasing t1 to 125nm from 100nm
Cutoff wavelength

## Slide 10: Flat Solar Cells: Manifestations of Fabry Perot Resonances
L=300nm
L=400nm
Killing FP ringings
Shifting FP peaks outside of cutoff wavelength
150/300
L=Ltouch

## Slide 11: Light trapping: Advantage of a nanodome
Flat layers
Dome case
metal
PbS
ZnO
metal
PbS
ZnO
Increasing optical length, wavefront shaping
Focusing
Increasing the absorber volume
Same effective
thickness: a jump
from 30 to 37 mA/cm2

## Slide 12: Light trapping: Advantage of a nanodome
L=Ltouch
High aspect ratio

## Slide 13: Light trapping: Advantage of a nanodome
AZO=>80nm
nSi=>300nm
NiO=>50nm
Au=>50nm
300nm
600nm
TiO2=>10nm
Au=>50nm
nSi=>300nm
NiO=>50nm
AZO=>80nm
300nm
600nm
TiO2=>10nm
light
light
Substrate configurations
Superstrate configurations

## Slide 14: Light trapping: Advantage of a nanodome
Short wavelengths

## Slide 15: Light trapping: Advantage of a nanodome

## Slide 16: Light trapping: Advantage of a nanodome
(E-field)2 @ 458nm – 650 THz | 
Substrate | Superstrate
All intensity plots are on the same scale

## Slide 17: Light trapping: Advantage of a nanodome
(E-field)2 @ 434nm – 690 THz | 
Substrate | Superstrate
All intensity plots are on the same scale

## Slide 18: Light trapping: Yablonovitch limit
Paper: E. Yablonovitch, J. Opt. Soc. Am. vol. 72, 899, 1982
light

## Slide 19: Light trapping: Yablonovitch limit
600-1500nm: 39.26mA/cm2
600-1000nm: 24.8mA/cm2
400-600nm: 11.84mA/cm2
aSi
CdTe
nSi
Yablonovitch limited absorption curves for h=250nm
Short wavelength
Long wavelength
Long wavelength
aSi: 7.3mA, 600-700nm
CdTe: 17.3mA, 600-850nm
nSi: 27.6mA 600-1050nm

## Slide 20: Light trapping: Yablonovitch limit
Absorber thickness | Jsc (mA/cm2)
25nm | 14.01
250nm | 17.61
500nm | 18.24
1000nm | 18.73
2000nm | 19.07
Mostly governed by short wavelength response
aSi

## Slide 21: Light trapping: Yablonovitch limit
nSi
Absorber thickness | Jsc (mA/cm2)
25nm | 23.1
250nm | 32.32
500nm | 34
1000nm | 35.33
2000nm | 36.37
Mostly governed by long wavelength response

## Slide 22: Light trapping: Yablonovitch limit
CdTe
Absorber thickness | Jsc (mA/cm2)
25nm | 22.12
250nm | 27.36
500nm | 27.93
1000nm | 28.31
2000nm | 28.54
Governed by short wavelength response

## Slide 23: Light trapping: Bloch modes
Slab modes
Air line
Even mode
Odd mode
(a)
Fig. 1
- Fig. 1 taken from: http://photonicswiki.org/index.php?title=File:Optical-fibre.svg
slab
k

## Slide 24: Light trapping: Bloch modes
Scatterer modes
Continous modes
Coupled to air
(b)
k

## Slide 25: Light trapping: Bloch modes
Even mode 1
Even mode 2
Odd mode
x
z

## Slide 26: Light trapping: Bloch modes
nSI
d1
L=300nm, w= 150nm, d2=200nm, d1=20nm (left), d1=100nm (middle), d1=200nm (right)
folding
Gets separated
Starts to get
separated
nSi (200nm)
air
L
w

## Slide 27: Light trapping: Bloch modes
nSI
d1
L=300nm, w= 150nm, d2=200nm, d1=20nm (left), d1=100nm (middle), d1=200nm (right)
nSi (200nm)
air
L
ZnO (80nm)
w
air

## Slide 28: Light trapping: Bloch modes
nSI
nSi (200nm)
air
L
w
air
ZnO (80nm)
d1
L=300nm, w= 150nm, d2=200nm, d1=20nm (left), d1=100nm (middle), d1=200nm (right)

## Slide 29: Light trapping: Bloch modes
nSI
d1
nSi (200nm)
air
L
w

## Slide 30: Light trapping: Bloch modes
Bloch modes
Air mode

## Slide 31: Light trapping: Diffraction aided Waveguiding
nSI
d2
nSi (200nm)
air
L
w
Light at normal incidence
Coupled tangential k
Incoming
tangential
Phase
term
Outgoing
tangential

## Slide 32: Light trapping: Diffraction aided Waveguiding
Diffraction order, mode number | Frequency (THz)
1st order diffraction, 1st mode | 282
1st order diffraction, 2nd mode | 369
1st order diffraction, 3rd mode | 496
1st order diffraction, 4th mode | 647
2nd order diffraction, 1st mode | 524
2nd order diffraction, 2nd mode | 587
perturbation

## Slide 33: Light trapping: Diffraction aided Waveguiding
Flat layers

## Slide 34: Light trapping: Diffraction aided Waveguiding
100 THz
200 THz
280 THz
363 THz
484 THz

## Slide 35: Light trapping: Diffraction aided Waveguiding
518 THz
579 THz
600 THz
624 THz

## Slide 36: Light trapping: Diffraction aided Waveguiding
nSI
d1
nSi (200nm)
air
L
ZnO (80nm)
w
Diffraction order, mode number | Frequency (THz)
1st order diffraction, 1st mode | 279
1st order diffraction, 2nd mode | 363
1st order diffraction, 3rd mode | 485
2nd order diffraction, 1st mode | 524
2nd order diffraction, 2nd mode | 585

## Slide 37: Light trapping: Mie resonances
AZO
nSi
nanowire
air

## Slide 38: Light trapping: Mie resonances
Without slab
Without slab
nSi slab
metal
nSi
nanowire
AZO

## Slide 39: Light trapping: Hybridization
1000nm nSi
AZO

## Slide 40: Light trapping: Hybridization
Mie/Bloch wave Hybridization

## Slide 41: Light trapping: Hybridization
Waveguiding

## Slide 42: Light trapping: Hybridization
Mie/Bloch wave Hybridization

## Slide 43: Light trapping: Hybridization
Mie Hybridization

## Slide 44: Light trapping: Hybridization
Smaller nanowire/dome
1
2
3
4

## Slide 45: Light trapping: Hybridization
Longer L

## Slide 46: Light trapping: Hybridization
ZnO
ncSi
ω
k
The effect of L spacing

## Slide 47: Light trapping: Hybridization
Shorter L

## Slide 48: Light trapping: Hybridization
Waveguide thickness

## Slide 49: Light trapping: Hybridization
ZnO
nc-Si
ω
k
The effect of waveguide thickness

## Slide 50: Light trapping: Hybridization

## Slide 51: Light trapping: Hybridization

## Slide 52: Light trapping: Hybridization

## Slide 53: Light trapping: Plasmonics
losses

## Slide 54: Light trapping: Plasmonics

## Slide 55: Examples: Mie Resonances
Fig. 2: “Broadband omnidirectional antireflection coating based on subwavelength surface Mie resonators” P. Spinelli, M. A. Verschuuren, A. Polman, Nature Comm. 3, 692 (2012).
Fig. 2
Introduction of a leaky channel into the substrate
cylinder
sphere

## Slide 56: Examples: Mie Resonances
Fig. 3
Fig. 3: “Broadband omnidirectional antireflection coating based on subwavelength surface Mie resonators” P. Spinelli, M. A. Verschuuren, A. Polman, Nature Comm. 3, 692 (2012).
Bare Si
With 60nm ARC
from 40o

## Slide 57: Examples: Mie Resonances
Fig. 4
Fig. 4: “Broadband omnidirectional antireflection coating based on subwavelength surface Mie resonators” P. Spinelli, M. A. Verschuuren, A. Polman, Nature Comm. 3, 692 (2012).
Red-shift
ARC tuned for UV-blue
Scattering after 800nm

## Slide 58: Examples: Hybridization
Fig. 5
Fig. 5: “Nanophotonics light trapping with patterned transparent conductive oxides” A. P. Vasudev, J. A. Schuller, M. L. Brongersma Optics Express 10, A385-A394 (2012).

## Slide 59: Examples: Hybridization
Fig. 6
Fig. 6: “Nanophotonics light trapping with patterned transparent conductive oxides” A. P. Vasudev, J. A. Schuller, M. L. Brongersma Optics Express 10, A385-A394 (2012).

## Slide 60: Examples: Hybridization
Fig. 7
Fig. 7: “Nanophotonics light trapping with patterned transparent conductive oxides” A. P. Vasudev, J. A. Schuller, M. L. Brongersma Optics Express 10, A385-A394 (2012).

## Slide 61: Examples: Hybridization
Fig. 8
Fig. 8: “Nanophotonics light trapping with patterned transparent conductive oxides” A. P. Vasudev, J. A. Schuller, M. L. Brongersma Optics Express 10, A385-A394 (2012).

## Slide 62: Examples: Plasmonics
Fig. 9
Fig. 9: “Light trapping in ultrathin plasmonic solar cells” V. E. Ferry, M. A. Verschuuren, H. B. T. Li, E. Verhagen, R. J. Walters, R. E. I. Schropp, H. A. Atwater, A. Polman Optics Express 18, A237-A245 (2010).

## Slide 63: Examples: Plasmonics
Fig. 10
Fig. 10: “Light trapping in ultrathin plasmonic solar cells” V. E. Ferry, M. A. Verschuuren, H. B. T. Li, E. Verhagen, R. J. Walters, R. E. I. Schropp, H. A. Atwater, A. Polman Optics Express 18, A237-A245 (2010).

## Slide 64: Examples: Plasmonics
Fig. 10
Fig. 10: “Light trapping in ultrathin plasmonic solar cells” V. E. Ferry, M. A. Verschuuren, H. B. T. Li, E. Verhagen, R. J. Walters, R. E. I. Schropp, H. A. Atwater, A. Polman Optics Express 18, A237-A245 (2010).

## Slide 65: Examples: Plasmonics
Fig. 11
Fig. 11: “Light trapping in ultrathin plasmonic solar cells” V. E. Ferry, M. A. Verschuuren, H. B. T. Li, E. Verhagen, R. J. Walters, R. E. I. Schropp, H. A. Atwater, A. Polman Optics Express 18, A237-A245 (2010).
measurement
simulation

## Slide 66: Examples: Plasmonics
Fig. 12
Fig. 12: “Light trapping in ultrathin plasmonic solar cells” V. E. Ferry, M. A. Verschuuren, H. B. T. Li, E. Verhagen, R. J. Walters, R. E. I. Schropp, H. A. Atwater, A. Polman Optics Express 18, A237-A245 (2010).

## Slide 67: Examples: Waveguiding
Fig. 13
Fig. 13: “Light Trapping in Solar Cells: Can Periodic Beat Random?” C. Battaglia, C.-M. Hsu, K. Soderstrom, J. Escarre, F.-J. Haug, M. Charriere, M. Boccard, M. Despeisse, D. T. L. Alexander, M. Cantoni, Y. Cui, C. Ballif ACS Nano 6, 2790-2797, 2012.

## Slide 68: Examples: Waveguiding
Diffraction peaks
Fig. 14
Fig. 14: “Light Trapping in Solar Cells: Can Periodic Beat Random?” C. Battaglia, C.-M. Hsu, K. Soderstrom, J. Escarre, F.-J. Haug, M. Charriere, M. Boccard, M. Despeisse, D. T. L. Alexander, M. Cantoni, Y. Cui, C. Ballif ACS Nano 6, 2790-2797, 2012.

## Slide 69: Examples: Waveguiding
Most of the power is here
Fig. 15
Fig. 15: “Light Trapping in Solar Cells: Can Periodic Beat Random?” C. Battaglia, C.-M. Hsu, K. Soderstrom, J. Escarre, F.-J. Haug, M. Charriere, M. Boccard, M. Despeisse, D. T. L. Alexander, M. Cantoni, Y. Cui, C. Ballif ACS Nano 6, 2790-2797, 2012.

## Slide 70: Examples: Waveguiding
Fig. 16
Fig. 16: “Light Trapping in Solar Cells: Can Periodic Beat Random?” C. Battaglia, C.-M. Hsu, K. Soderstrom, J. Escarre, F.-J. Haug, M. Charriere, M. Boccard, M. Despeisse, D. T. L. Alexander, M. Cantoni, Y. Cui, C. Ballif ACS Nano 6, 2790-2797, 2012.

## Slide 71: Examples: Photonic Crystals
Fig. 17
Fig. 17: “Light Trapping in ultrathin silicon photonic crystal superlattices with randomly-textured dielectric incouplers” D. M. Callahan, K. A. W. Horowitz, H. A. Atwater Optics Express 21, 30315-30326 (2013).

## Slide 72: Examples: Photonic Crystals
Fig. 18
Fig. 18: “Light Trapping in ultrathin silicon photonic crystal superlattices with randomly-textured dielectric incouplers” D. M. Callahan, K. A. W. Horowitz, H. A. Atwater Optics Express 21, 30315-30326 (2013).

## Slide 73: Examples: Photonic Crystals
Fig. 19
Fig. 19: “Light Trapping in ultrathin silicon photonic crystal superlattices with randomly-textured dielectric incouplers” D. M. Callahan, K. A. W. Horowitz, H. A. Atwater Optics Express 21, 30315-30326 (2013).

## Slide 74: Examples: Photonic Crystals
Fig. 20
Fig. 20: “Light Trapping in ultrathin silicon photonic crystal superlattices with randomly-textured dielectric incouplers” D. M. Callahan, K. A. W. Horowitz, H. A. Atwater Optics Express 21, 30315-30326 (2013).

## Slide 75: Examples: Photonic Crystals
Fig. 21
Fig. 21: “Light Trapping in ultrathin silicon photonic crystal superlattices with randomly-textured dielectric incouplers” D. M. Callahan, K. A. W. Horowitz, H. A. Atwater Optics Express 21, 30315-30326 (2013).

## Slide 76: Examples: Photonic Crystals
Fig. 22
Fig. 22: “Light Trapping in ultrathin silicon photonic crystal superlattices with randomly-textured dielectric incouplers” D. M. Callahan, K. A. W. Horowitz, H. A. Atwater Optics Express 21, 30315-30326 (2013).