## Slide 1
Plasma Removal Process

## Slide 2: Outline
Introduction
Models to understand the plasma process
Chemistry
Analyzing recipe parameters, and the resultant etch profiles
Endpoint

## Slide 3: Sidewall Passivation
Sidewall passivation can be used in an etch process to control sidewall profile
A film forms on the sidewalls, preventing the material from being etched isotropically
The film is actually a polymer formed from the process gases and the photoresist layer on the substrate
The polymers are basically combinations of carbon and hydrogen. May contain oxygen and nitrogen and other etch byproducts. Polymer chemistry depends on process conditions.
Specific gases can be added to the recipe to insure passivation film formation

## Slide 4: Etch Profile with Sidewall Passivation
Radicals: reactive etching species
Reaction Products: volatile etch products
Film formers: provide sidewall passivation, photoresist can be a large contributor
Positive ions: provide physical bombardment on surface, breaking surface film formers at bottom, physically etching and providing energy to help drive chemical reactions
Public Domain: Image Generated by CNEU Staff for free use

## Slide 5: Sidewall Passivation
Polymers coat the sidewalls and act as a “pseudo-mask” for protection from chemical attack
Ions, for the most part, strike vertically and remove polymer buildup at the bottom of the etch
The sidewall polymers are removed by using O2 plasma at 500-750mT
  This exposure uses a lot of chemistry and little bombardment

## Slide 6
Outline
Introduction
Models to understand the plasma process
Chemistry
Analyzing recipe parameters, and the resultant etch profiles
Endpoint

## Slide 7
Controlling the Etch Process by Balancing Chemistry and Bombardment
In dry etch processes choosing the correct chemistries can greatly increase the etch rate
Increasing MFP of the plasma (decreasing the pressure) also increases the etch rate, this will aid uniformity
Combining chemistry and bombardment will produce an etch rate that is greater than either contributor alone
Combining chemistry and bombardment allows the profile to be “tuned” between isotropic and anisotropic
The etch profile can also be enhanced with side wall passivation

## Slide 8: Example Sidewall Chemistries
Material | Chemistry | Volatile Etch Product | Sidewall Material
Oxide Etch | SiO2 + CF4 + CHF3 + Ar  | SiF, SiOF, SiF4, SiH4 | Si, C, CHx, F 
Poly Si Etch | Si + HBr + Cl2  | SiBrx  SiClx | Si,Br,C,Cl 
Al Etch | Al + BCl3 + Cl2 + N2  | AlCl3  | Al,B,C,N,Cl 

## Slide 9
Formula | Common Name | Chemical Name | Formula | Chemical Name
CF4 | Freon 14 | Tetrafluoro-methane | SiCl4 | Silicon Tetrachloride
C2F6 | Freon 116 | Perfluoro-ethane | BCl3 | Boron-trichloride
C3F8 | Freon 218 | Perfluoro-propane | Cl2 | Chlorine
CHF3 | Freon 23 | Trifluoro-methane | HCl | Hydrogen Chloride
CF3Br | Freon 13B1 | Bromo- trifluoro-methane | HBr | Hydrogen Bromide
SF6 |  | Sulfur Hexafluoride | He | Helium
NF3 |  | Nitrogen Trifluoride | N2 | Nitrogen
SiF4 |  | Silicon Tetrafluoride | O2 | Oxygen
Some etching Gases

## Slide 10
PolySilicon | Cl2 or BCl3/CCl4 HBr /CF4 /CHCl3 /CHF3 | WSi2,TiSi2,CoSi2 | CCl2F3
Aluminum | Cl2 BCl3 + passivating gases SiCl4 | Single crystal Si | Cl2 or BCl3 + passivating gases
AlSi(1%)-Cu(0.5%) | same as Al | SiO2 (BPSG) | CCl2F2,CF4,C2F6, C3F8
Al-Cu(2%) | BCl3/Cl2/CHF3 | Si3N4 | CCl2F2 CHF3
Tungsten | SF6/Cl2/CCl4 | GaAs | CCl2F2
TiW | SF6/Cl2/O2 |  | 
Material
Chemistry
Chemistry
Material
Some Materials and Selected Etchants

## Slide 11
Outline
Introduction
Models to understand the plasma process
Chemistry
Analyzing recipe parameters and the resultant etch profiles
Endpoint

## Slide 12: The “Egg” Chart
This analytical model is a graphical representation of various process parameters. The Y axis represents bombardment energy, the X axis represents chemical energy, and the “dog leg” boundary represents polymer formation.
For an ideal anisotropic etch, the required parameter zone resembles an “egg” in the middle of the chart
This chart shows the combined effects of chemistry, bombardment, and polymerization (C*B+P) to predict sidewall profiles
There are also other factors that determine the etch profile that are not included in this exercise. These parameters will be discussed after this first iteration analysis.

## Slide 13: The “Egg” Chart
A chart like this can be found and/or generated for any dry etchable material
Due to its wide use in micro and nanofabrication, we will analyze the egg chart for SiO2
Naturally this chart is not “exact”, but can be used as a starting point for building a etch recipe.

## Slide 14: Oxide Egg Chart Considerations
F/C Ratio- the ratio of fluorine to carbon etching species
Increasing DC bias, increases bombardment
The addition of H2 to the chamber increases polymerization
The addition of O2 to the chamber increases free fluorine
Aspect Ratio- the ratio of depth to width for a small gap, trench, or hole

## Slide 15
0
1
2
3
4
Fluorine to Carbon Ratio (F/C) of Gas Phase Etching Species vs DC Bias Level
Bias Applied to Surface (Volts)
DC Bias
Low
High
Polymerization
Etching
O2 Addition
Loading
H2 Addition
C2F4
C4F10
C2F6
CF4
F/C Ratio
Public Domain: Image Generated by CNEU Staff for free use

## Slide 16
0
1
2
3
4
Fluorine to Carbon Ratio (F/C) of Gas Phase Etching Species vs DC Bias Level
Bias Applied to Surface (Volts)
DC Bias
Low
High
Polymerization
Etching
O2 Addition
Loading
H2 Addition
C2F4
C4F10
C2F6
CF4
F/C Ratio
Public Domain: Image Generated by CNEU Staff for free use
1

## Slide 17: The Ideal Profile
To be “in the egg” is to achieve the ideal anisotropic etch
  The ideal F/C ratio is approximately 2
  An equal mix of hydrogen and oxygen to balance polymerization and etch
  DC bias level that provides just enough bombardment

## Slide 18: The Ideal Profile
D
W
Public Domain: Image Generated by CNEU Staff for free use

## Slide 19: Sidewall Profile Two
Low DC bias – little/no bombardment
No H2 - no polymerization
A lot of O2 – can increase etching
F/C ratio = 4, SiF4 is formed
Aspect ratio < 1, an isotropic etch profile

## Slide 20
0
1
2
3
4
Fluorine to Carbon Ratio (F/C) of Gas Phase Etching Species vs DC Bias Level
Bias Applied to Surface (Volts)
DC Bias
Low
High
Polymerization
Etching
O2 Addition
Loading
H2 Addition
C2F4
C4F10
C2F6
CF4
F/C Ratio
Public Domain: Image Generated by CNEU Staff for free use
2

## Slide 21: Sidewall Profile Two
Public Domain: Image Generated by CNEU Staff for free use

## Slide 22: Sidewall Profile Three
Low DC bias – no bombardment
A lot of H2 - a lot of polymerization
No O2 – no etch
F/C = 1/3, SiF4 is not formed

## Slide 23
0
1
2
3
4
Fluorine to Carbon Ratio (F/C) of Gas Phase Etching Species vs DC Bias Level
Bias Applied to Surface (Volts)
DC Bias
Low
High
Polymerization
Etching
O2 Addition
Loading
H2 Addition
C2F4
C4F10
C2F6
CF4
F/C Ratio
Public Domain: Image Generated by CNEU Staff for free use
3

## Slide 24: Sidewall Profile Three
Polymer buildup
Public Domain: Image Generated by CNEU Staff for free use

## Slide 25: Sidewall Profile Four
High DC bias – high bombardment
No H2 – no polymerization
A lot of O2 – high etch
F/C ratio = 4, SiF4 is formed
Aspect ratio >1, a dry etch profile

## Slide 26
0
1
2
3
4
Fluorine to Carbon Ratio (F/C) of Gas Phase Etching Species vs DC Bias Level
Bias Applied to Surface (Volts)
DC Bias
Low
High
Polymerization
Etching
O2 Addition
Loading
H2 Addition
C2F4
C4F10
C2F6
CF4
F/C Ratio
Public Domain: Image Generated by CNEU Staff for free use
4

## Slide 27: Sidewall Profile Four
6
3
Sharp angles due
to high bombardment
with no polymerization
Public Domain: Image Generated by CNEU Staff for free use

## Slide 28: Sidewall Profile Five
High DC bias – high bombardment
A lot of H2 – a lot of polymerization
No O2 – no etch
F/C ratio =1/5, SiF4 is not formed
Aspect ratio > 1, Dry etch profile with undesirable features

## Slide 29
0
1
2
3
4
Fluorine to Carbon Ratio (F/C) of Gas Phase Etching Species vs DC Bias Level
Bias Applied to Surface (Volts)
DC Bias
Low
High
Polymerization
Etching
O2 Addition
Loading
H2 Addition
C2F4
C4F10
C2F6
CF4
F/C Ratio
Public Domain: Image Generated by CNEU Staff for free use
5

## Slide 30: Sidewall Profile Five
Jagged features
due to
polymer buildup
Public Domain: Image Generated by CNEU Staff for free use

## Slide 31: Sidewall Profile Six
Medium DC bias – medium bombardment
No H2 – no polymerization
A lot of O2 – high etch
F/C = 4, SiF4 is formed
Aspect ratio < 1, a wet etch profile

## Slide 32
0
1
2
3
4
Fluorine to Carbon Ratio (F/C) of Gas Phase Etching Species vs DC Bias Level
Bias Applied to Surface (Volts)
DC Bias
Low
High
Polymerization
Etching
O2 Addition
Loading
H2 Addition
C2F4
C4F10
C2F6
CF4
F/C Ratio
6
Public Domain: Image Generated by CNEU Staff for free use

## Slide 33: Sidewall Profile Six
Wider and deeper
than profile one
due to increased
bombardment
Public Domain: Image Generated by CNEU Staff for free use

## Slide 34: Sidewall Profile Seven
Medium DC bias – medium bombardment
A lot of H2 – a lot of polymerization
No O2 – no etch
F/C ratio = ¼, SiF4 is not formed
Aspect ratio > 1, Dry etch profile with undesirable features

## Slide 35
0
1
2
3
4
Fluorine to Carbon Ratio (F/C) of Gas Phase Etching Species vs DC Bias Level
Bias Applied to Surface (Volts)
DC Bias
Low
High
Polymerization
Etching
O2 Addition
Loading
H2 Addition
C2F4
C4F10
C2F6
CF4
F/C Ratio
7
Public Domain: Image Generated by CNEU Staff for free use

## Slide 36: Sidewall Profile Seven
Less bombardment than profile four
Public Domain: Image Generated by CNEU Staff for free use

## Slide 37
Considerations Beyond
the Egg Chart
The “egg chart” is a useful first approximation to define some process parameters, but it does not cover some important considerations.
We will discuss 4 additional considerations:
  Residence time
  Microloading
  Proximity effect
  Post etch evaluation

## Slide 38
Residence Time
The average time gas is present in the chamber (seconds)
The residence time is a balance of the pressure, input gas flow, and the pump efficiency
Naturally the residence time will impact the etch process, because etch chemistry and byproducts are constantly being pumped away at a certain rate

## Slide 39
Microloading
The change in local etch rate relative to the whole area of material being etched
  A large area will load the etching process with volatile etch products, slowing the etch down in that area while a smaller etch area proceeds at a faster rate
Etch rates change according to pattern and exposed area

## Slide 40
Microloading
Larger area loading
the process with removed
material- less etching gas
relative to area
More etching
gas relative to area-
etches quicker
Photoresist on top of Wafer
Patterned holes in the PR where etching of the wafer occurs
Public Domain: Image Generated by CNEU Staff for free use

## Slide 41
Proximity Effect- Etch Rate Based on Feature Size
Si
Si
F
SiF4
“Crowded”-
harder to remove byproducts,
slower etch rate
Si
Si
F
SiF4
Easier to remove byproducts,
faster etch rate
Public Domain: Image Generated by CNEU Staff for free use

## Slide 42
Etch Evaluation
Process quality parameters:
  Etch rate, selectivity, uniformity
  Sidewall Profile
  Loss or gain of critical dimensions
  Corrosion (in metal etch)
  Reproducibility

## Slide 43
Outline
Introduction
Models to understand the plasma process
Chemistry
Analyzing recipe parameters, and the resultant etch profiles
Endpoint

## Slide 44: Endpoint Detection
General term describing when an etch process has finished
Two common methods of detection
  Optical emission
  Mass spectroscopy

## Slide 45: Optical Emission
Each volatile etch product emits a specific wavelength
The wavelength intensity shows the relative amounts of products being formed
A decrease in intensity corresponds to a decrease in etch products.

## Slide 46: RIE With Optical Endpoint Detector
Endpoint Detector
Oxford Instruments Plasmalab System 100
Public Domain: Image Generated by CNEU Staff for free use

## Slide 47
Optical Emission
Material to be etched | Etchant Gases | Emitting Species | (nm)
Silicon | CF4/O2; SF | F(product) | 704
 | CF4/O2; SF | SiF(product) | 440, 777
 | Cl2 | SiCl(product) | 287
SiO2 | CHF3 | CO(product) | 484
Si3N4 | CF4/O2 | N2(product) | 337
 | CF4/O2 | CN(product) | 387
 | CF4/O2 | N(product) | 674
 | CF4/O2 | F(etchant) | 704
Al | Cl2; BCl3 | Al(product) | 391, 394, 396
 | Cl2; BCl3 | AlCl(product) | 261
Resist | O2 | O(etchant) | 777, 843
 | O2 | CO(product) | 484
 | O2 | OH(product) | 309
 | O2 | H(product) | 656

## Slide 48: Example Graph of Optical Endpoint Detection
Endpoint detection
Normal etch
Change in etch rate - detection occurs here.
Endpoint signal stops the etch.
Time
Etch Parameter
Public Domain: Image Generated by CNEU Staff for free use

## Slide 49: Mass Spectroscopy
This method of endpoint detection measures the mass/charge ratio of the etch products
As the mass/charge ratio peak declines, the products being generated by the etch decline due to the material being etched away
A residual gas analyzer is a mass spectrometer

## Slide 50: Mass Spectrometer Schematic
Detector
Steering magnets
Particle Accelerator
Ionizing electron stream
A
Public Domain: Image Generated by CNEU Staff for free use

## Slide 51: Example Mass Spectra: Benzyl Alcohol
Benzyl Alcohol
Public Domain: Image Generated by CNEU Staff for free use