## Slide 1
Understanding Variation and Statistical Process Control:
Process Variation and Statistical Process Control (SPC)

## Slide 2: Outline
Normal and Special Cause Variation
Specification Limits vs Control Limits
Calculations for the Individuals Chart.
Nelson Rules to determine out-of-control signals (special cause variation) from process data.
Calculations for the X bar & R Chart.
Advantages of subgroup data collection.

## Slide 3: Corning Process to Manufacture Gorilla Glass
Quality = Strong, flexible, scratch resistant.

## Slide 4: Measuring the Compression Layer in Glass
The quality of the ultra-thin glass used for phones and tablets is a function of the compression induced strength developed from the ion exchange treatment. With this compression, comes a band of tension just inside the compressive edge. It is important that this tension not exceed limits or flow too far into the glass where a simple scratch or check can turn into a run away crack. Gauges use the polarization of light passing through the glass to measure the level of compression / tension.
Distance (nm)
SnapDatInc copyright 2014

## Slide 5: Responding to Variation in the Process
1/2/14 0
1/2/14 8
1/2/14 16
1/3/14 0
1/3/14 8
1/3/14 16
1/4/14 0
1/4/14 8
1/4/14 16
1/5/14 0
1/5/14 8
1/5/14 16
1/6/14 0
3.2
3.0
2.8
2.6
2.4
2.2
Date
SnapDatInc copyright 2014
Strain
Lower Spec
Upper Spec
Target
Glass Strain (MPascal) over Time
Wait for the next 4 hr sample
Take another measurement
Shut down & adjust process
Adjust minor input

## Slide 6: Responding to Variation in the Process
1/2014 0
1/2014 8
1/2014 16
1/2014 0
1/2014 8
1/2014 16
1/2014 0
1/2014 8
1/2014 16
1/2014 0
1/2014 8
1/2014 16
1/2014 0
3.50
3.25
3.00
2.75
2.50
2.25
2.00
Date
SnapDatInc copyright 2014
Strain
Target
Upper Spec
Lower Spec
Glass Strain (MPascal) over Time
Wait for the next 4 hr sample
Take another measurement
Shut down & adjust process
Adjust minor input

## Slide 7: Limits to the Process vs Specification Limits
Wait for the next 4 hr sample
Take another measurement
Shut down & adjust process
Adjust minor input
12/29/13 16
12/30/1 3 0
12/30/13 8
12/30/13 16
12/31/13 0
12/31/13 8
1 2/31/13 16
1/1/14 0
1/1/14 8
1/1/14 16
1/2/14 0
1/2/1 4 8
1/2/14 16
1/3/14 0
1/3/14 8
1/3/14 16
1/4/1 4 0
1/4/14 8
1/4/14 16
1/5/14 0
1/5/14 8
1/5/14 16
1/6/14 0
3.4
3.2
3.0
2.8
2.6
2.4
Date
SnapDatInc copyright 2014
Strain
Upper Spec 2
2.2
Lower Spec 2
2.0
Lower Spec
Upper Spec
Target
Glass Strain (MPascal) over Time

## Slide 8: Limits to the Process vs Specification Limits
Wait for the next 4 hr sample
Take another measurement
Shut down & adjust process
Adjust minor input
12/29/13 16
12/30/1 3 0
12/30/13 8
12/30/13 16
12/31/13 0
12/31/13 8
1 2/31/13 16
1/1/14 0
1/1/14 8
1/1/14 16
1/2/14 0
1/2/1 4 8
1/2/14 16
1/3/14 0
1/3/14 8
1/3/14 16
1/4/1 4 0
1/4/14 8
1/4/14 16
1/5/14 0
1/5/14 8
1/5/14 16
1/6/14 0
3.4
3.2
3.0
2.8
2.6
2.4
Date
SnapDatInc copyright 2014
Strain
Target
Upper Spec
Lower Spec
2.2
Lower Spec 2
2.0
Upper Spec 2
Glass Strain (MPascal) over Time

## Slide 9: Histogram of the Glass Strain Data
3.2
3.0
2.8
2.4
2.2
2.0
10
8
6
4
2
0
Mean 2.635
StDev 0.2017
N 44
2.6
Strain
Frequency
Lower Control Limit
Histogram of Glass Strain
Normal
Upper Control Limit

## Slide 10: Histogram Converted to a Control Chart
46
41
36
31
16
11
6
1
3.2
3.0
2.8
2.6
2.4
2.2
2.0
21 26
Observation
Glass Strain
_ X=2.638
UCL=3.171
LCL=2.105
Individuals Chart of Glass Strain

## Slide 11: Characteristics of a Control Chart
Control Chart – a time series plot for process monitoring which allows one to tell common cause variation from special cause variation by identifying the natural variation in the process with control limits.
Control Limits – a range of values that contain the natural variation of the process. One must collect process data and calculate the standard deviation to determine the control limits.
  Data within the control limits is normal variation. One data point outside the limits must have been caused by something special.
  Control charts also test each data point for the formation of patterns which would not occur under normal random variation. Any of these eight patterns indicate that something special occurred, beyond normal random variation.

## Slide 12: Sources of Variation – Time to Drive to Work
Stoplights in your favor (or not).
Slow driver in front of you.
Have to drop off your spouse at their work (or not).
Forgot; wallet, keys, coffee mug, phone, daughter, etc.
Flat tire.
Number of cars on the road (congestion).
Construction on your typical route.
You’re in the mood for some speed.
Accident; other guy’s fault, of course.

## Slide 13: Sources of Variation – Common or Special?
Non-normal Variation, Does not follow a bell curve
Out-of-control
Larger changes
Fast (spike)
Often, single known source
Does not occur most of the time
Can not be predicted
8. Most likely, you should respond and fix
1. Normal Variation, Follows a bell curve
In-control, stable
Smaller changes
Slow (drift)
Unknown source, sum of many small contributors
Occurs all the time
Can be quantified as having a certain size
Responding will most likely make it worse
Special Cause Variation Common Cause Variation

## Slide 14
Identifying Special Cause Variation
What patterns in the data in the copper concentration shown below seem to identify special cause variation in the average copper concentration?

## Slide 15: Additional Unusual or Non-random Patterns
In 1984, Lloyd Nelson published 8 patterns that you won’t seen in the data if there is only normal random variation at play. These are based on the original Shewhart 5 patterns which later became the Western Electric 6 patterns. Some more commonly used tests are;
Lloyd S. Nelson, “Technical Aid”, Journal of Quality Technology, Vol.16, No.4, 1984, p238-239

## Slide 16: Additional Unusual or Non-random Patterns
In 1984, Lloyd Nelson published 8 patterns that you won’t seen in the data if there is only normal random variation at play. These are based on the original Shewhart 5 patterns which later became the Western Electric 6 patterns. Some more commonly used tests are;
Lloyd S. Nelson, “Technical Aid”, Journal of Quality Technology, Vol.16, No.4, 1984, p238-239
SnapDatInc copyright 2013

## Slide 17: Determining Patterns from Special Cause Variation
1 2 3 4 5 6 7
15.6
15.4
15.2
15.0
14.8
14.6
14.4
14.2
15.6
15.4
15.2
15.0
14.8
14.6
14.4
14.2
14.0
1 2 3 4 5 6 7
15.5
15.0
14.5
14.0
13.5
13.0
1 2 3 4 5 6 7
Time
Paint Viscosity Over Time
** Montgomery, Douglas (2005)) , Introduction to Statistical Quality Control, 5th Edition
4 points*Point
Common
5 points*Point
Not Uncommon
6 points*Point
Special Cause
How common is each pattern?
6 points trending will only occur about .27% ** of the time under normal random variation.
Test 3

## Slide 18: Eight Tests for Special Cause Variation
The probability that any one of these 8 patterns will be seen in the data if there is only normal random variation is very low. Therefore, if one of these patterns is seen, it was likely caused by a special source of variation.

## Slide 19: Identifying Special Cause Variation with 8 Tests
What patterns in the data shown below seem to identify special cause variation in the average copper concentration?

## Slide 20: Identifying Special Cause Variation with 8 Tests
1/6/14 4
1/5/14 8
1/4/14 12
1/3/14 16
1/2/14 20
1/2/14 0
1/1/14 4
12/31/13 8
12/30/13 12
12/29/13 16
3.2
3.0
2.8
2.6
2.4
2.2
2.0
Date
Glass Strain
_ X=2.630
UCL=3.179
LCL=2.081
6
5
Individuals Chart of Glass Strain

## Slide 21: Dry Etch Process for Microprocessor Mfg
Isotropic
Anisotropic
Dry etch technology has been greatly refined for today’s advanced fabrication of integrated circuits. One etch quality characteristic that affects the performance of the semiconductor product is anisotropy, a high level of vertical etching vs horizontal etching. This is measured as the aspect ratio, the depth / the width of the etched area.
Problem: The aspect ratio of grooves from the dry etch process should have an aspect ratio of 1.00, but can vary from .9 to 1.1 and still meet specifications. Five wafers are sampled every 4 hours and the aspect ratio is measured to monitor the quality of the product from the etch process.

## Slide 22: Value of Collecting Subgroup Data
Range2/Mean2
SnapDatInc copyright 2013
Subgroup 2
Range3/Mean3
Subgroup 3
Range4/Mean4
Subgroup 4
Create an X-bar (Mean) and R (Range) Chart
Range1/Mean1 Subgroup 1

## Slide 23: X-bar & R Chart of the Process
46
41
36
31
21
16
11
6
1
1.050
1.025
1.000
0.975
0.950
26
Sample
Sample Mean
_ X=1.0030
UCL=1.0433
LCL=0.9626
46
41
36
31
21
16
11
6
1
0.16
0.12
0.08
0.04
0.00
26
Sample
Sample Range
_ R=0.0699
UCL=0.1479
LCL=0
1
1
6
5
2
1
Xbar-R Chart of Aspect Ratio

## Slide 24: Identification of Out-of Control Subgroups
Test Results for Xbar Chart of Aspect Ratio
TEST 1. One point more than 3.00 standard deviations from center line. Test Failed at points: 25, 47
TEST 5. 2 out of 3 points more than 2 standard deviations from center line (on one side of CL).
Test Failed at points: 7
TEST 6. 4 out of 5 points more than 1 standard deviation from center line (on one side of CL).
Test Failed at points: 10
Test Results for R Chart of Aspect Ratio
TEST 1. One point more than 3.00 standard deviations from center line. Test Failed at points: 11
TEST 2. 9 points in a row on same side of center line. Test Failed at points: 29
* WARNING * If graph is updated with new data, the results above may no
* longer be correct.

## Slide 25: Advantages of the X-bar & R Chart over Individuals
Lower Variation – Clear Picture
Standard Deviation of the Average
Standard Deviation
of the Individuals Sqrt (N )
Means are Normal – the Central Limit Theorem dictates that the mean of several measurements will follow a normal distribution even if the individual readings do not. Normality is assumed for the 8 tests.
Monitor the Mean and Variation –
the X-bar chart monitors the
center of the process distribution while the R or S chart monitors the variability. Both are important.
=
SnapDatInc copyright 2014

## Slide 26: When to use the I- Chart
Individuals Control Chart (I-MR )
Used when monitoring is a single continuous process.
Common application; long, expensive or difficult measurement .
Works best with low measurement variation.
Works best with normally distributed data.

## Slide 27: The Xbar and S Chart
10/20 8pm
10/20 12am
10/19 4am
10/18 8am
10/17 12pm
10/16 4pm
10/15 8pm
10/15 12am
10/14 4am
10/13 8am
1.050
1.025
1.000
0.975
0.950
Date/Time
Sample Mean
_ X=1.0030
UCL=1.0435
LCL=0.9625
10/20 8pm
10/20 12am
10/19 4am
10/18 8am
10/17 12pm
10/16 4pm
10/15 8pm
10/15 12am
10/14 4am
10/13 8am
0.060
0.045
0.030
0.015
0.000
Date/Time
Sample StDev
_ S=0.02837
UCL=0.05927
LCL=0
1
1
6
5
2
2
1
Xbar-S Chart of Aspect Ratio

## Slide 28: When to use the S Chart
Xbar - S Control Chart
Used when you have a calculator or computer generated chart.
Equivalent to an X-bar & R with small subgroup sizes (5 or less) .
Right choice for subgroup size 9 or larger.
Right choice for unequal subgroup size.

## Slide 29: Conclusions
The complexity of modern nanoscale processes demand accurate control plans that minimize the false alarms and detect changes to the process that require remediation. Control charts are a key tool in these plans.
Control limits define the normal variation in the process which does not require follow-up and distinguishes it from the special cause variation that should be addressed.
Eight patterns in the response data from your process have been identified as having a low probability of occurrence without a special cause. Modern software can be used to identify these patterns in your data to trigger an appropriate response.
If process data is collected in subgroups and analyzed using control charts for subgrouped data, the sensitivity of the chart to special cause variation and the information about the process are improved over the standard control chart of individual data points.

## Slide 30: References
Automotive Industry Action Group, (2005). Statistical Process Control 2nd Edition . AIAG Press, Detroit, MI.
Hoyer, Robert W. and Ellis, Wayne C., “A Graphical Exploration of SPC”, Quality Progress, May,1996, p65-73.
Lloyd S. Nelson, “Technical Aid”, Journal of Quality Technology,
Vol.16, No.4, 1984, p238-239.
Montgomery, Douglas (2005). Introduction to Statistical Quality Control , 5th Edition. John Wiley & Sons Inc. Hoboken NJ.
Wheeler, Donald J. and Chambers, David S. (1992). Understanding Statistical Process Control. SPC Press: Knoxville, TN.