## Slide 1
Introduction to Nanotechnology
Module #6
How Do You Make Things So Small?
An Introduction to Nanofabrication
Nanotechnology is Impacting Everything
© patton brothers illustration (www.pattonbros.com)
Copyright April 2009 The Pennsylvania State University
Last Updated: 1/6/2011
Notes: <number>
There is a glossary that comes along with this set of modules. Each term in blue print in every module is defined in this glossary.

## Slide 2
  This module is one of a series designed to be used by faculty members at post-secondary institutions in workshops, courses, and overview lectures to introduce nanotechnology and its applications. There is no particular significance to the module number system
  The series was funded in part by:
  The National Science Foundation
  Grant # DUE 0532646 and DUE 0802498
  and
  The Pennsylvania Department of Community and Economic Development
  Grant # C000029471 and C000036659
  Any opinions, findings, and conclusions or recommendations expressed in this material are those of the author and do not necessarily reflect the views of the National Science Foundation or the Pennsylvania Department of Community and Economic Development
Copyright April 2009 The Pennsylvania State University

## Slide 3: Glossary of Terms
Throughout these modules you will find words and terms printed in the color blue. These words and terms are defined in the glossary (glossary.html), which can be opened by clicking here.
Copyright April 2009 The Pennsylvania State University

## Slide 4: Outline
What is nanofabrication
What is made by nanofabrication and how
How is nanofabrication directed
An overview of top-down and bottom-up nanofabrication
Top-down nanofabrication
Bottom-up nanofabrication
Key points
Copyright April 2009 The Pennsylvania State University

## Slide 5: Outline
What is nanofabrication
What is made by nanofabrication and how
How is nanofabrication directed
An overview of top-down and bottom-up nanofabrication
Top-down nanofabrication
Bottom-up nanofabrication
Key points
Copyright April 2009 The Pennsylvania State University

## Slide 6: Making nano-scale “things” is called Nanofabrication
Copyright April 2009 The Pennsylvania State University

## Slide 7
There are three different approaches to Nanofabrication –
    Top-down nanofabrication
    Bottom-up nanofabrication
    Hybrid nanofabrication
Copyright April 2009 The Pennsylvania State University

## Slide 8: Outline
What is nanofabrication
What is made by nanofabrication and how
How is nanofabrication directed
An overview of top-down and bottom-up nanofabrication
Top-down nanofabrication
Bottom-up nanofabrication
Key points
Copyright April 2009 The Pennsylvania State University

## Slide 9
        Nano-particles
        (e.g., macro-molecules,
        beads, tubes, wires)
        Planar structures
        (e.g., structures built
        using layers)
        Hybrid structures (mixtures of particles
        and planar structures)
Nanotechnology uses Nanofabrication to make a wide variety of Nano-structures –
Copyright April 2009 The Pennsylvania State University
Evidenttech.com
Adapted from Linda Geppert, The Amazing Vanishing Transistor Act,
IEEE Spectrum, October 2002, Vol. 39, Number 10, pg. 28-33

## Slide 10
How are these things made –
    Top-down nanofabrication makes nano-structures by repeated use of steps that put down films and take parts of them away
    Bottom-up nanofabrication builds up nano-structures from atoms, molecules, particles, or some combination of these
    Hybrid nanofabrication combines elements of top-down and bottom-up nanofabrication
Copyright April 2009 The Pennsylvania State University

## Slide 11: Outline
What is nanofabrication.
What is made by nanofabrication and how
How is nanofabrication directed
An overview of top-down and bottom-up nanofabrication
Top-down nanofabrication
Bottom-up nanofabrication
Key points
Copyright April 2009 The Pennsylvania State University

## Slide 12
Sometimes no direction is
needed; i.e., no patterns for
establishing positioning are
required (e.g., nanoparticles in solution)
Sometimes direction is required; i.e.,
sometimes patterns for positioning are
necessary (e.g., transistors on a
substrate)
No external pattern control
Hybrid
How do you direct Nanofabrication?
Copyright April 2009 The Pennsylvania State University
Evidenttech.com
Adapted from Linda Geppert, The Amazing Vanishing Transistor Act,
IEEE Spectrum, October 2002, Vol. 39, Number 10, pg. 28-33

## Slide 13
Externally Imposed Pattern (This
approach is generally called
lithography)
Inherent Pattern (Uses size,
shape, or chemical bonding to
impose patterning)
Hybrid (mixture of both)
No external pattern control
Hybrid
When Pattern Controlled Fabrication is required, it can utilize an-
Copyright April 2009 The Pennsylvania State University

## Slide 14
Using lithography for placing, growing, or modifying materials into patterns, where you want, on a structure on a substrate
Using lithography for removing materials, where you don’t want them, on a structure on a substrate
External Patterning means-
Copyright April 2009 The Pennsylvania State University

## Slide 15: An Example of An Externally Imposed Pattern (Lithography)
Pattern is transferred from a “mask” using light (photolithography) in this example
Pattern is external to structure. It is originally here (on what is called a “mask”)
Pattern is transferred to here (in this case by using a material that is sensitive to light)
Fabrication is done here following the transferred pattern
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU

## Slide 16
Using size, shape, specific chemical bonding or all of these to establish a pattern in the nanofabrication
No external pattern control
Hybrid
Inherent Patterning means-
Copyright April 2009 The Pennsylvania State University

## Slide 17: An Example of An Inherent Pattern
Pattern is dictated by shape and chemical bonding in this example
Antigen “fits” into antibody due to shape, size, and specific chemical bonding and self-assembles
Antigen Antibody
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU

## Slide 18: Outline
What is nanofabrication
What is made by nanofabrication and how
How is nanofabrication directed
An overview of top-down and bottom-up nanofabrication
Top-down nanofabrication
Bottom-up nanofabrication
Key points
Copyright April 2009 The Pennsylvania State University

## Slide 19: Top-down Nanofabrication is like Sculpting
Start with a material supported on
a substrate
Add some new material
according to a pattern (lithography)
Copyright April 2009 The Pennsylvania State University
Image courtesy of Bruce Hirst
Image courtesy of Bruce Hirst

## Slide 20: Top-down Nanofabrication is like Sculpting
Subtract some of the material according to a pattern (Process order is not important; can subtract before or after adding)
Repeat the adding/subtracting as
needed following the pattern
Copyright April 2009 The Pennsylvania State University
Image courtesy of Bruce Hirst
Image courtesy of Bruce Hirst
Notes: <number>
Following this sculpting analogy, the modification step could be coloring the eyes blue.

## Slide 21: Bottom-up Nanofabrication is like putting blocks together
The building blocks can go together in some inherent
pattern dictated by shape or
they can go together randomly.
The building blocks can be atoms, molecules, or nanoparticles
Copyright April 2009 The Pennsylvania State University
Notes: <number>
Following this sculpting analogy, the modification step could be coloring the eyes blue.

## Slide 22: Top-Down Vs. Bottom-Up Nanofabrication
Top-Down Nanofabrication
In “top-down” nanofabrication, one grows or deposits layers of materials and, by some combination of physical and chemical methods, creates the desired nanostructure, as you would make a statue from a block of marble. Top-down nanotechnology is based on the methods that are used to make microelectronics chips; i.e., structures of carefully controlled, limited dimensions are created by laying down layers of material, modifying properties as needed, and etching away those parts of each layer that are unwanted. These steps are guided by lithography.
Bottom-Up Nanofabrication
In “bottom-up” nanofabrication approaches, one starts with small components – for example, individual molecules and nano-particles – and then assembles these components to make the desired structure. Often the assembly is self-guiding; i.e., self-assembly.
Copyright April 2009 The Pennsylvania State University

## Slide 23
The basic materials of top-down nanofabrication are layers (e.g., films) of materials.
The basic materials of bottom-up nanofabrication are atoms, molecules, particles, and layers.
Copyright April 2009 The Pennsylvania State University

## Slide 24: Outline
What is nanofabrication
What is made by nanofabrication and how
How is nanofabrication directed
An overview of top-down and bottom-up nanofabrication
Top-down nanofabrication
Bottom-up nanofabrication
Key points
Copyright April 2009 The Pennsylvania State University

## Slide 25
  Lithography (Pattern transfer)
  Growth/Deposition (Addition process)
  Etching (Subtraction process)
  Modification
  No external pattern control
  Hybrid
Top-down Nanofabrication always
uses some combination of-
Copyright April 2009 The Pennsylvania State University

## Slide 26: Here’s the way Top-down Nanofabricaton is done –
The four steps (lithography, addition, subtraction and modification) are use in some sequence.
Steps may be skipped. You can start with any step.
The sequence usually starts with growth or deposition of material.
Lithography is the step which orchestrates all the others. It controls where materials stay and where they are “sculpted” (i.e., etched) away.
Copyright April 2009 The Pennsylvania State University

## Slide 27
Etching
Lithography
Depositing
or
Growing
Material
Modification
The Top-down Fabrication Methodology
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU

## Slide 28
Let’s see an example of how top-down nanofabrication is used to make nano-scale structures.
Copyright April 2009 The Pennsylvania State University

## Slide 29: An Example of a Top-Down Nanofabrication Processing Sequence
Copyright April 2009 The Pennsylvania State University
Film Grown by Chemical Reaction of Ambient species with the Substrate
Thin Film
Substrate
Photoresist
Mask
PLASMA ETCH
+
IONS
+
IONS
+
IONS
LITHOGRAPHY
ETCHING
Chemistry
Chemistry
Chemistry
Spin on Photoresist
Align Photomask
Expose with Light
Chemical Bonds are Altered in Exposed Areas
Dissolve Exposed Photoresist in Liquid Developer
Remove the Photoresist (Etch/Ion Implantation) Barrier
(Negative Bias)
Pattern Transfer and Substrate Modification Complete
HEAT
Substrate
THIN FILM GROWTH OR DEPOSITION
Oxygen
SURFACE MODIFICATION
+
+
+
+
+
+
+
Ion Implantation
Thermal Anneal
HEAT
Notes: <number>

## Slide 30: The preceding cartoon demonstrates the four basic steps of top-down nanofabrication:
Growth or deposition (addition)
Lithography (pattern transfer)
Etching (subtraction)
Material modification (to change electrical, optical, mechanical, or chemical properties in some region of a layer)
Copyright April 2009 The Pennsylvania State University

## Slide 31: Outline
What is nanofabrication
What is made by nanofabrication and how
How is nanofabrication directed
An overview of top-down and bottom-up nanofabrication
Top-down nanofabrication
Bottom-up nanofabrication
Key points
Copyright April 2009 The Pennsylvania State University

## Slide 32
Bottom-up Nanofabrication always uses some combination of –
Building block (molecules, particles, and layers) fabrication
Self-assembly
Copyright April 2009 The Pennsylvania State University

## Slide 33: Here’s the way Bottom-up Nanofabricaton is done –
The two steps (building block fabrication and self-assembly) are used in some sequence.
Steps may be skipped.
The sequence starts with building block fabrication .
An inherent patterning process (due to size, shape, chemical bonding) may be present.
Copyright April 2009 The Pennsylvania State University

## Slide 34
Building
Block
Fabrication
Self
Assembly
The Bottom-up Fabrication Methodology
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU

## Slide 35
Let’s see an example of how
bottom-up nanofabrication is used
to make nano-scale structures
Copyright April 2009 The Pennsylvania State University

## Slide 36
An Example of a Bottom-Up Nanofabrication Processing Sequence
Functionalize the Nanoparticle
Link with Antibodies
Antigen Attachment
Synthesize Nanoparticle
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU
Notes: <number>

## Slide 37: The preceding cartoon demonstrates the two basic steps of bottom-up nanofabrication:
Building Block Fabrication (molecules, particles, or layers--the basic building blocks of bottom-up nanofabrication)
Assembly of the building blocks into functioning nanostructures. This step is usually termed self-assembly
In this example, an inherent pattern was present dictated by allowed chemical bonds
Copyright April 2009 The Pennsylvania State University

## Slide 38: Outline
What is nanofabrication
What is made by nanofabrication and how
How is nanofabrication directed
An overview of top-down and bottom-up nanofabrication
Top-down nanofabrication
Bottom-up nanofabrication
Key points
Copyright April 2009 The Pennsylvania State University

## Slide 39: Key Points
The making of Nanostructures is termed Nanofabrication
There are two types of Nanofabrication: (1) Top-down and (2) Bottom-up nanofabrication
The combination of the two is called Hybrid nanofabrication
Copyright April 2009 The Pennsylvania State University

## Slide 40: Key Points (Continued)
4. Top-down makes structures from layers using addition/subtraction processes guided by a pattern established by lithography. Material modification steps may also be included
5. Top-down nanotechnology is based on the methods that are used to make microelectronics chips; i.e., structures of carefully controlled, limited dimensions are created by laying down layers of material and etching away those parts of each layer that are unwanted. These steps are guided by lithography
Copyright April 2009 The Pennsylvania State University

## Slide 41: Key Points (Continued)
6. Bottom-up assembles building blocks. It can be random or it can follow an inherent pattern present due to bonding, size, or shape
7. Bottom-up uses atoms, molecules and nano-particles and self-assembles these components to make the desired structure
Copyright April 2009 The Pennsylvania State University

## Slide 42
This module, produced by the Center for Nanotechnology Education and Utilization at
The Pennsylvania State University,
is one of a series developed to introduce nanotechnology and its applications to a broad audience. Each module, its component viewgraphs, and the companion glossary are copyrighted 2009 by
The Pennsylvania State University.
All rights reserved.
Copyright April 2009 The Pennsylvania State University