## Slide 1
Introduction to Nanotechnology
Module #8
How Do You Build Things So Small:
Bottom-Up Nanofabrication
Nanotechnology is Impacting Everything
© patton brothers illustration (www.pattonbros.com)
Copyright April 2009 The Pennsylvania State University
Last Updated: 1/6/2011
Notes: <number>
There is a glossary that comes along with this set of modules. Each term in blue print in every module is defined in this glossary.

## Slide 2
  This module is one of a series designed to be used by faculty members at post-secondary institutions in workshops, courses, and overview lectures to introduce nanotechnology and its applications. There is no particular significance to the module number system
  The series was funded in part by:
  The National Science Foundation
  Grant # DUE 0532646 and DUE 0802598
  and
  The Pennsylvania Department of Community and Economic Development
  Grant # C000029471 and C000036659
  Any opinions, findings, and conclusions or recommendations expressed in this material are those of the author and do not necessarily reflect the views of the National Science Foundation or the Pennsylvania Department of Community and Economic Development
Copyright April 2009 The Pennsylvania State University

## Slide 3: Glossary of Terms
Throughout these modules you will find words and terms printed in the color blue. These words and terms are defined in the glossary (glossary.html), which can be opened by clicking here.
Copyright April 2009 The Pennsylvania State University

## Slide 4: Outline
The basic approach of bottom-up nanofabrication
The basic steps
Building block fabrication approaches
Self assembly
Summary
Key Ideas
Copyright April 2009 The Pennsylvania State University
Notes: <number>
The instructor may want to break this module into two lectures. There`s a lot of material here.

## Slide 5: Outline
The basic approach of bottom-up nanofabrication
The basic steps
Building block fabrication approaches
Self assembly
Summary
Key Ideas
Copyright April 2009 The Pennsylvania State University
Notes: <number>
The instructor may want to break this module into two lectures. There`s a lot of material here.

## Slide 6: Bottom-Up Nanofabrication
Starts with small components – for example, individual molecules and nano-particles – and which are then assembled to make the desired structure.
Copyright April 2009 The Pennsylvania State University

## Slide 7: Bottom-up Nanofabrication is like putting blocks together
The building blocks can go together in some inherent pattern dictated by shape or they can go together randomly
The building blocks can be atoms,
molecules, or nanoparticles
Copyright April 2009 The Pennsylvania State University
Notes: <number>
Following this sculpting analogy, the modification step could be coloring the eyes blue.

## Slide 8: Outline
The basic approach of bottom-up nanofabrication
The basic steps
Building block fabrication approaches
Self assembly
Summary
Key Ideas
Copyright April 2009 The Pennsylvania State University
Notes: <number>
The instructor may want to break this module into two lectures. There`s a lot of material here.

## Slide 9: Nanofabrication can be considered to have two basic steps:
Building Block Fabrication (making the molecules, particles, or layers--the basic building blocks of bottom-up nanofabrication)
Assembly of the building blocks
into functioning nanostructures. This step is usually termed self-assembly
Copyright April 2009 The Pennsylvania State University

## Slide 10
Building Block
Fabrication
Assembly
The Bottom-down Fabrication Methodology
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU

## Slide 11: Here’s the way bottom-up nanofabricaton is usually done –
The building blocks (molecules, particles, layers) are
fabricated
These building blocks self assemble into a
nanostructure for some nanotechnology application
Building block fabrication and assembly may occur in
one step
The sequence may be repeated many times
The resulting nanostructures may reside in a solution,
on a surface, or in an object
There is no use of the lithography or etching steps
orchestrating what goes where; hence the use of the
term “self-assembly”
Copyright April 2009 The Pennsylvania State University

## Slide 12
We now examine some building block fabrication and assembly approaches.
Copyright April 2009 The Pennsylvania State University

## Slide 13: Outline
The basic approach of bottom-up nanofabrication
The basic steps
Building block fabrication approaches
Self assembly
Summary
Key Ideas
Copyright April 2009 The Pennsylvania State University
Notes: <number>
The instructor may want to break this module into two lectures. There`s a lot of material here.

## Slide 14
Building Block Fabrication
Some of the possible building block fabrication approaches include:
  Molecule synthesis
  Colloidal chemistry
  Physical fabrication approaches
  Chemical vapor growth
Copyright April 2009 The Pennsylvania State University

## Slide 15: Molecule Synthesis
Copyright April 2009 The Pennsylvania State University

## Slide 16: Molecules Synthesized for Linking
Tail Group – selected to
bind to specific materials,
particles, molecules
Body of the molecule.
Actual atom arrangement
of this molecule
Molecules made with a tail group (green ball) to give functionality; i.e., used to dictate what the molecule will bond to. Head group (not shown) can then dictate what the molecule links to at its other end.
S
H2C
H2C
CH2
H2C
CH2
CH2
CH2
H2C
CH2
H2C
CH3
H2C
Example: the sulfur tail group of the alkanethiolate molecule
Copyright April 2009 The Pennsylvania State University

## Slide 17
Macromolecule synthesis For example, a dendrimer is a 3-D macromolecule that is synthesized by a series of reactions creating layers (See G1, G2, etc. below). Dendrimers can then be functionalized (at Z’s) for linking and/or attachment.
“Commercializing Nanotechnology”, NATURE BIOTECHNOLOGY Volume 21, Number 10, October 2003
Copyright April 2009 The Pennsylvania State University

## Slide 18: Colloidal chemistry (solution chemistry)
Copyright April 2009 The Pennsylvania State University

## Slide 19
By setting up carefully controlled reactions in a solution, atoms and molecules can be assembled, using colloidal chemistry, to make nanoparticles.
It is a great way to make nanoparticles such as metal nanoparticles and quantum dots.
Colloidal chemistry methods are by far the most commonly used to produce low cost bulk quantities of nanoparticles, nanoclusters and quantum dots.
Copyright April 2009 The Pennsylvania State University

## Slide 20: Colloidal Chemistry
The general procedure involves chemical reactions in aqueous or nonaqueous solutions containing soluble or suspended salts, which are one of the precursors. Once the solution becomes supersaturated with the product of the chemical reaction involving the precursors, the precipitate (nanoparticles) start to form by nucleation and growth.
precursor
precursor
solvent
reaction
Supersaturation of solution and production of nanoparticles
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU

## Slide 21
Thiophenolate results in the formation of capping layer stopping growth
and limiting nanoparticle size
CdS
Example: CdS quantum dots
Cd
Cd
S
CdS
S
Average cluster size can be controlled by simply adjusting the ratio of sulphite to additive thiophenolate in solution
Control of growth rate/particle size
Copyright April 2009 The Pennsylvania State University
For the production of CdS quantum dots by colloidal chemistry, a solution of cadmium chloride is reduced by sodium sulfide
Molecules can be put into the solution which bind to the surface these types of coating molecules are used to control nanoparticle size
When the nanoparticle reaches a specified size, these coating molecules from a stable coating and hinder further growth
J. Mater. Sci. 1997, 32, 245.

## Slide 22: Physical Approaches
Copyright April 2009 The Pennsylvania State University

## Slide 23: Physical approaches
Techniques used for producing metal and metal oxide
nanoparticles using physical approaches include: Vapor condensation and mechanical processes
such as grinding or milling.
Vapor Condensation:
By utilizing either an inert atmosphere for metallic nanoparticles or
an oxygen rich atmosphere for metal oxides, solid nanoparticles
can be formed when a metal vapor is rapidly condensed. By varying the temperature, gas flow and vapor production rate, precise nanoparticle sizes can be obtained.
Grinding or Milling: Nanoparticles are created by mechanical size reduction. The
properties of the resulting nanoparticles are dependent upon
the starting material, grinding/milling time, and the processing
ambient. This method gives limited control of resulting
nanoparticle sizes as well as limited control of contamination.
Copyright April 2009 The Pennsylvania State University

## Slide 24: Chemical Vapor Growth
Copyright April 2009 The Pennsylvania State University

## Slide 25
An Example: Carbon Nanotubes (CNTs) grown from methane gas decomposition at iron nanoparticle catalysts
Copyright April 2009 The Pennsylvania State University
“Carbon nanotube films obtained by thermal chemical vapour deposition”. Journal of Materials Chemistry. Oleg A. Nerushev , Martin Sveningsson , Lena K. L. Falk and Frank Rohmund. March 2001. http://dx.doi.org/10.1039/DOI – Reproduced by permission of The Royal Society of Chemistry

## Slide 26: Another Example: silicon nanowires produced by chemical vapor growth using the Vapor-Liquid-Solid (VLS) mechanism
Gold nanoparticle becomes supersaturated
with Si which then precipitates out as a solid nanowire.(shown in green)
Gold (Au) nanoparticles are positioned on a substrate
Nanoparticles act as a catalyst releasing silicon (Si) from its precursor (source). Si then dissolves into the gold
The Si Nanowire (SiNW) has a diameter dictated by the size of the Au nanoparticle
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU

## Slide 27: Another Example: Silicon/germanium Nanowires produced by chemical vapor growth using the Vapor-Liquid-Solid (VLS) mechanism
Silicon/germanium (SiGe)
alloy nanowires
Kok-Keong Lew, Ling Pan, Elizabeth C. Dickey, Joan M .Redwing:. Vapor-Liquid-Solid Growth of Silicon- Germanium Nanowires. Advanced Materials. 2003. Vol.15(24), pages 2073-2074. Copyright Wiley-VCH Verlag GmbH & Co. KGaA. Reproduced with permission.
Copyright April 2009 The Pennsylvania State University

## Slide 28: Outline
The basic approach of bottom-up nanofabrication
The basic steps
Building block fabrication approaches
Self assembly
Summary
Key Ideas
Copyright April 2009 The Pennsylvania State University
Notes: <number>
The instructor may want to break this module into two lectures. There`s a lot of material here.

## Slide 29
Self Assembly
Self assembly involves one of the following:
  Chemical assembly
  Physical assembly
  Biological assembly
Copyright April 2009 The Pennsylvania State University

## Slide 30: Chemical Self Assembly
Copyright April 2009 The Pennsylvania State University
  In this example, alkanethiol molecules form a self-assembled monolayer (SAM) on a gold surface
  Selected alkanethiols can have useful functional groups at their free head ends
  Therefore, thiols can chemically modify a surface and even allow for molecular recognition (sensors)
Gold Surface
Receptors
Thiol
Solution
Adsorption
SAM
Courtesy of CNEU
Notes: <number>

## Slide 31
Physical Self-Assembly
  In this example, an applied electric field causes conducting carbon nanotubes in a slurry to stand up
Carbon nanotubes assembled into this vertical orientation by an electric field
Copyright April 2009 The Pennsylvania State University
“Vertical alignment of printed carbon nanotubes by multiple field emission cycles” Yong C. Kim, K. H. Sohn, Y. M. Cho, and Eun H. Yoo. Volume 84, issue 26. page 5351. © 2004 American Institute of Physics

## Slide 32: Biological Self Assembly In this example, DNA is used to link gold nanoparticles together
Chad Mirkin (Northwestern University)
Copyright April 2009 The Pennsylvania State University

## Slide 33: Outline
The basic approach of bottom-up nanofabrication
The basic steps
Building block fabrication approaches
Self assembly
Summary
Key Ideas
Copyright April 2009 The Pennsylvania State University
Notes: <number>
The instructor may want to break this module into two lectures. There`s a lot of material here.

## Slide 34
We just completed looking at the two processes used in bottom-up nanofabrication: building block fabrication and self-assembly.
Now let’s run an example sequence where these steps are put together to create a nanostructure.
The answer to the question of what such structures could be used for lies in the mind and in the creativity of the person who designs the bottom-up nanofabrication sequence.
Copyright April 2009 The Pennsylvania State University

## Slide 35
An Example of a Bottom-Up Nanofabrication Processing Sequence
Functionalize the Nanoparticle
Link with Antibodies
Antigen Attachment
Synthesize Nanoparticle
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU
Notes: <number>

## Slide 36: Outline
The basic approach of bottom-up nanofabrication
The basic steps
Building block fabrication approaches
Self assembly
Summary
Key Ideas
Copyright April 2009 The Pennsylvania State University
Notes: <number>
The instructor may want to break this module into two lectures. There`s a lot of material here.

## Slide 37
Key Ideas
There are two processes in bottom-up nanofabrication: building block fabrication and self-assembly
The building blocks used include molecules, particles (beads, wires, tubes), and layers
The building block fabrication approaches include molecule synthesis, colloidal chemistry, physical approaches, and chemical vapor growth
Copyright April 2009 The Pennsylvania State University

## Slide 38
Key Ideas (continued)
The self-assembly approaches include chemical, physical, and biological self assembly
Lithography and etching steps are not part of bottom-up nanofabrication
The bottom-up nanofabrication approach mimics the way nature tends to make things—start small and add
Copyright April 2009 The Pennsylvania State University

## Slide 39
This module, produced by the Center for Nanotechnology Education and Utilization at
The Pennsylvania State University,
is one of a series developed to introduce nanotechnology and its applications to a broad audience. Each module, its component viewgraphs, and the companion glossary are copyrighted 2009 by
The Pennsylvania State University.
All rights reserved.
Copyright April 2009 The Pennsylvania State University